FU TEN DUO INDUSTRIAL CORP.

PP/PE Monofilament Making Machine

| SPECIFICATION: | Model | FTD-55 | FTD-65 | FTD-75 |
| --- | --- | --- | --- | --- |
| Feature | Material | HDPE or PP |
|  | Product Diameter | Ø0.15 mm ~ Ø0.40mm |
|  | Extruding Capacity | 15~30kg/hr | 30~60kg/hr | 40~70kg/hr |
| Extruder | Screw Dia. | Ø55mm | Ø65mm | Ø75mm |
|  | Screw L/D | 24/1 | 24/1 | 28/1 |
|  | Screw Material | ALLOY STEEL |
|  | Barrel Material | ALLOY STEEL |
|  | Heater Capacity | 10 KW | 18 KW | 24 KW |
|  | Driving Motor | 20 HP | 30 HP | 40 HP |
|  | Hopper Loader | Option | 1 SET | 1 SET |
| Control Panel | Temp. Control | 4 ZONES | 5 ZONES | 6 ZONES |
| Cooling Device | Cooling type | WATER COOLING TANK |
| Take-off unit (A) | Type | 8 PCS OF ROLLER |
|  | Driving Motor | 2 HP | 3 HP | 5 HP |
| Stretching Device | Type | HOT WATER |
|  | Heater Capacity | 8 KW | 12 KW | 16 KW |
| Take-off unit (B) | Type | 8 PCS OF ROLLER |
|  | Driving Motor | 3 HP | 5 HP | 7 1/2 HP |
| Annealing Device | Type | HOT AIR CIRCULATION |
|  | Heater Capacity | 18 KW | 24 KW | 30 KW |
| Take-off unit (C) | Type | 8 PCS OF ROLLER |
|  | Driving Motor | 3 HP | 5 HP | 7 1/2 HP |
| Winding unit | Type | DIRECT |
|  | Number of Beam | 84 PCS | 124 PCS | 150 PCS |
|  | Driving Motor | 2 HP HYDRAULIC MOTOR |
| Dimension | LxWxH (M) | 16 x 2 x 2.5 | 17 x 2 x 2.5 | 18 x 2 x 2.5 |

NYLON Monofilament Making Machine.

| Other Products: Blown Film Machine PVC & Rigid, Soft Profile Extruder Machine. Flat Yarn Machine Laminating Machine & Straw making Machine. Plastic Roofing Plank & Plank Making Machine. Wire Covering Machine. Granule-Machine, for Treatment of plastic Waste. PP Heavy-duty Packing Tape Making machine. 9. Plastic Machinery of Extrusion System. |  |  |
| --- | --- | --- |