FU TEN DUO INDUSTRIAL CORP.

Computerised Cold Feed Type Rubber Preformer

Item No.FTD-25CCF

Specification:

| Extrusion Volume | 25 Liter |
| --- | --- |
| Main Power | 220Vx3, 60HZ, 75HP |
| Vacuum Pump | 220/380, 3Ø. 60HZ, 0.55KW |
| Extrusion Speed | 01~15mm/sec. |
| Extrusion Cylinder Diameter | Ø200 mm |
| Pressure on compound | 2840 PSI |
| Preform weight Min/Max. | 0.25G~3.0G |
| Weight Tolerance | 1.5% |
| O.D. of Product’s Size | Ø170 mm Max. |
| Cutting Speed(double Knives) | 500 cuts/min Max. |
| Machine Head | Ø185 mm |
| Tempering System | Water tempering unit: 2 sets |
| Machine Weight | Approx 5300kg |
| Machine Size (LxWxH) | 470cmx200cmx215cm |