| ### Item | ### Product | ### Material | ### Hardness (HRC) | ### Diameter (mm) | ### Length (mm) | ### Head | ### Point | ### Surface Treatment |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Y-13A | washered steel nail | Steel | 54° ~ 57° | 3.7 | 25 ~ 75 | flat) | needle | Zinc Plating |
| Y-13B | washered steel nail | Steel | 54° ~ 57° | 3.7 | 25 ~ 75 | flat | needle | Zinc Plating |
| Y-13C | washered steel nail | Steel | 54° ~ 57° | 3.7 | 25 ~ 75 | flat | needle | Zinc Plating |
| Y-13D | washered steel nail | Steel | 54° ~ 57° | 2.5~3.7 | 25 ~ 75 | flat | needle | Zinc Plating |
| Y-13E | washered steel nail | Steel | 54° ~ 57° | 2.5~3.6 | 25 ~ 75 | flat | needle | Zinc Plating |